## Slide 1
Presented by: Matilde Matos
SUPERCONDUCTING
CABLES AND TAPES
1

## Slide 2
OVERVIEW
Superconductivity
01
Overview of SC Tapes
02
04
05
03
Conclusions
06
Overview of SC
Cables
Applications of SC
Tapes and Cables
Future
Outlooks
2

## Slide 3
1933 that physicists became aware of the other property of superconductors - perfect diamagnetism.
This was when Meissner and Oschenfeld discovered that a superconducting material cooled below its critical temperature in a magnetic field excluded the magnetic flux. This effect has now become known as the Meissner effect.
01 SUPERCONDUCTIVITY
In 1911, Kamerlingh-Onnes discovered that the electrical resistance of mercury goes to zero below 4.2 K (-269°C). This was the very first observation of the phenomenon of superconductivity.
DISCOVERY
MEISSNER EFFECT
3

## Slide 4
Materials were found that superconduct above 77K (the melting point of liquid nitrogen which is safer and more economic than liquid helium as a refrigerant).
01 SUPERCONDUCTIVITY
Conventional physics and the quantum theory of solid state are not capable of accurately explaining the superconducting state. In 1957 three american researchers (John Bardeen, Leon Cooper and John Schrieffer) established the microscopic theory of superconductivity.
BCS THEORY
HIGH TEMPERATURE SUPERCONDUCTION
4

## Slide 5
02 MATERIALS OF SC TAPES
HTS
LTS
Substrates and
Stabilizers
Insulating Layers
Buffer Layers
YBCO:
Often deposited in thin film form on a substrate
BSCCO:
Common material, especially in the form of multifilamentary
NbTi:
Especially used in applications like MRI
Nb3Sn:
Has higher Tc than NbTi, making it suitable for applications like high-field magnets
Metals:
Provide mechanical support and help dissipate heat
Rare Earth Elements:
Added to enhance the mechanical properties and stability
MgO:
Essential to prevent electrical shorts between the SC layers and the substrate
CeO2:
Used to promote the growth of high quality SC films and improve their performance
5

## Slide 6
02 MANUFACTURE OF SC TAPES
Starts with the electropolishing of a metallic substrate (usually hastelloid) in an acid bath to a surface roughness of around 1nm. Several layers are then deposited to form the buffer layers needed to achieve an epitaxial growth of the HTS film.
  Electropolishing
6
Notes: "Epitaxial" refers to a type of crystal growth where a thin layer of material is deposited on a crystalline substrate in such a way that the layer follows the crystallographic orientation of the substrate.

## Slide 7
02 MANUFACTURE OF SC TAPES
The aluminium is the first layer and its sputtered usually in the same chamber as the next layer, the yttrium.
2. Magnetron Sputtering
7

## Slide 8
02 MANUFACTURE OF SC TAPES
After that in an ion beam assisted deposition chamber an epitaxial magnesium oxide layer is deposited.
3. Ion Beam Assisted Deposition
8

## Slide 9
02 MANUFACTURE OF SC TAPES
At high temperatures a homoepitaxial magnesium oxide layer is then deposited followed by lanthanum manganite layer to provide robustness to the film and to match the lattice parameters of the HTS.
4. Magnetron Sputtering
9
Notes: Homoepitaxial: epitaxial layer is made of the same material as the substrate. This process involves depositing a thin film of the same crystalline material onto a substrate, ensuring that the deposited layer inherits the crystallographic orientation of the underlying material.

## Slide 10
02 MANUFACTURE OF SC TAPES
The HTS layer REBCO is then deposited using metalorganic chemical vapor deposition (MOCVD) machine at around 870 degrees. This thick layer is responsible for the zero resistivity at cryogenic temperatures.
5. Metalorganic Chemical Vapor Deposition
10

## Slide 11
02 MANUFACTURE OF SC TAPES
A silver layer is then deposited to protect the HTS layer. This layer also serves as a low resistivity electrical contact.
6. Magnetron Sputtering
11

## Slide 12
02 MANUFACTURE OF SC TAPES
A copper layer is electroplated in a chemical bath on both sides of the tape. This layer acts as a shunt layer.
7. Electropolishing
12

## Slide 13
03 SC CABLES
OVERVIEW
The HTS cables are placed in a pipe with vacuum (cryogen) which thermally isolates the superconductor from the remaining environment. They carry five times the current of a conventional cable system and they do not emit any heat to the environment. The technology requires special cable joints and specific cable termination for extreme temperature differences and permanent cooling for keeping cryostat.
13

## Slide 14
03 SC CABLE CONSTRUCTION
This image is an example of a sc cables construction and includes the following components:
  Conductor: Bi-based SC wires spirally laid on a former
  Electrical Insulation: Polypropylene Laminated Paper (PPLP) for its insulation and low dielectric loss at low temperatures
  Coolant: Liquid Nitrogen
  Shield Layer: SC wire of the same conductor material wound spirally outside the insulation layer and connected at both ends of the cable, inducing reverse electrical current to cancel EM field leakage
  Housing: Double-layred SUS corrugated piping with thermal insulation.
14
Notes: SUS: corrugated stainless steel tubing or piping. "Corrugated" refers to a surface that is shaped into a series of parallel ridges and grooves.

## Slide 15
03 CABLE DESGIN
Warm dielectric design
Based on a conductor, cooled by the flow of liquid nitrogen surrounded by a cryogenic envelope using two concentric flexible stainless steel tubes with vacuum and superinsulation in between
Cold dielectric design
The liquid nitrogen is used as a part of the dielectric system. Although more ambitious to manufacture, the cold configuration has the advantage of containing the electromagnetic field inside the superconducting screen, which significantly reduces the cable inductance.
15

## Slide 16
Superconducting cable can transmit electric power at an effective current density of over 100 A/mm2 . This allows high-capacity power transmission over the cables with more compact size than conventional cables, which makes it possible to greatly reduce construction costs.
Low Impact on
the Environment
Compactness and High Capacity
A superconductor system also has a smaller footprint in an underground installation as a result of not requiring large separation between cables.
03 ADVANTAGES OF SC CABLES
Low Transmission
Loss
In superconducting cables, the electrical resistance is zero at temperatures below the critical temperature, so its transmission loss is very small.
16

## Slide 17
04 APPLICATIONS OF SC TAPES AND CABLES
Power Transmission
Magnetic Ressonance Imaging (MRI)
Particle Accelerators
Fusion Energy Research
Superconducting cables can transmit large amounts of electricity over long distances with minimal energy loss, making them ideal for urban power grids and long-distance power transmission.
Advances in superconducting tape technology are enabling the development of more compact and portable MRI systems, expanding their accessibility and use in remote locations.
Superconducting cables are essential in building high-field magnets used in particle accelerators, which are crucial for advanced scientific research in physics.
Superconducting magnets are critical components in fusion reactors, such as tokamaks and stellarators, which aim to provide a sustainable and virtually limitless source of energy.
17

## Slide 18
04 APPLICATIONS OF SC TAPES AND CABLES
Fujikura Ltd. has delivered mass-production volumes of rare-earth-based HTS tapes to Commonwealth Fusion Systems (CFS), which is building the world's first commercially relevant fusion machine in the United States and has begun expanding production capacity for these tapes. The mission is to deploy fusion power plants to meet global decarbonization goals as fast as possible.
The Shingal Project is a 1 km 23 kV AC HTS cable connecting the 154 kV substations of Shingal and Heungdeok. This project used HTS cable with 50 km of HTS tape used.
The system was able to share the supply capacity between the two substations and this led to further research.
18

## Slide 19
FUTURE OUTLOOKS AND POTENTIAL BREAKTHROUGH
Room Temperature
Superconductors
Flexible SC Tapes
Compact Cable Designs
Advancements in materials science are enabling the development of HTS who can operate at less extreme cryogenic temperatures, reducing the complexity and cost of cooling systems. Eventually reaching room temperature superconductors
Innovative fabrication techniques are producing highly flexible SC tapes, expanding the range of applications and making installation in small spaces more feasible
Advances in SC materials and cryogenic engineering are eneabling the creation of more compact, high-capacity cable designs that can be easily integrated into existing infrastructures
19

## Slide 20
The End!
20